## Slide 1
The Utility Company of the Solar System
ACME - Final Review

## Slide 2: Table of contents
Project objectives and schedule
Proof of Concept
Breadboard design
Breadboard testing
Next steps
Conclusions

## Slide 3: ACME for Lunar Night Survival
Accelerated Combustion of Metals for Exothermic Heating
3

## Slide 4: Objectives of the activity
The objective of the activity was to investigate the use of metallothermic (thermite) reactions from reactant(s) available in lunar regolith to produce energy to potentially survive the lunar night.
PART A
Proof of Concept
PART B
Breadboard design and testing
Literature review and trade-off studies.
First experimental proof of the concept.
Requirements definition
Design of the breadboard
Integration of the breadboard
Testing of the breadboard
The activity was implemented through OSIP and structured in two parts:

## Slide 5: ACME schedule
Chart: 
| Total duration | Kickoff Meeting | Literature review and trade off | Proof of concept | Proof of Concept Review (MS1) | Reactor design | Design review | Procurement and manufacturing | Test Readiness Review (MS2) | Testing | Project Management | Final Review
START DATE | 44603 | 44603 | 44604 | 44683 | 44775 | 44743 | 44805 | 44806 | 44958 | 44959 | 44603 | 45152
DURATION (days) | 544 | 1 | 80 | 90 | 1 | 60 | 1 | 149 | 1 | 193 | 544 | 1
Except for some small deviations, the activity has been carried out following the initial schedule.

## Slide 6
PROOF OF CONCEPT

## Slide 7: ACME concept
+ Heat
Accelerated Combustion of Metals for Exothermic Heating
ACME
RECOVERY
MINING
+ 850 kJ
ENERGY
HEAT

## Slide 8: Use case definition
Mission | Energy cycle [kWh] | Energy mission [kWh]
Lander | 10.5 | 31.5
Rover | 10.5 | 125
Pressurized habitat | 219 | 25500
Data retrieved from “TN1 - Lunar Night Survival Requirements Derivation and Specification”, HERACLES-RIBRE-RP-0021
  Habitat. Integration with metals refinement from slag, beneficiation of regolith and resupply operations.
  Lander. Launching only metal reactant, equivalent energy density for reaction becomes 3600 Wh/kg (Si). Only reactions with raw regolith can be considered (no beneficiation capabilities assumed).
Rover. Even launching only metal reactant, impossible to meet 400 Wh/kg for 12 lunar nights (total 4800 Wh/kg).
HEX
LOADS
HEX
Radiators
ACME

## Slide 9: Reactions selection
Element | Highland [wt%]
Si | 21.1%
Fe | 4%
Al | 14.4%
Ca | 11.3%
Mg | 3.5%
Reaction | Score
Al + regolith | 0.65
Al + anorthosite | 0.63
Al + enstatite | 0.63
Mg + regolith | 0.58
REACTION SELECTION
METALS ON MOON
MINERALS ON MOON
Notes: AHP Analytic hierarchy process. Figure of merit:
Energy density
Oxides abundance
Metals provision
Useful products
Testing complexity

## Slide 10: Ignition method selection
MG RIBBON
SPARKLER
WIRE COIL
MICROWAVES
CONCENTRATOR
LASER
Ignition method | Score
Magnesium ribbon | 0.24
Sparkler | 0.24
Microwaves | 0.27
Wire coil | 0.32
Solar concentrator | 0.63
Laser | 0.76
Notes: Consumables
Power
Mass
Complexity
Operability

## Slide 11: Proof of Concept - Breadboard
T1 – Coil outlet temperature
T2 – Tank temperature
T3 – Pump outlet temperature
T4 – Sand layer Temperature
T1
T2
T3
10l
T4

## Slide 12: Proof of Concept - Reactions
Oxide source | Reducing material | Oxide source % | Reducing material % | Ignition/propagation | Speed of reaction | Grade of reaction
LMS-1 | Al | 80 | 20 | No | - | 0%
LMS-1 | Al | 70 | 30 | Yes | Slow | 90%
LMS-1 | Al | 60 | 40 | Yes | Medium | 95%
LMS-1 | Al | 50 | 50 | Yes | Medium | 95%
LHS-1 | Al | 80 | 20 | No | - | 0%
LHS-1 | Al | 70 | 30 | Yes | Slow | 80%
LHS-1 | Al | 60 | 40 | Yes | Slow | 90%
LHS-1 | Al | 50 | 50 | Yes | Medium | 90%
Anorthosite | Al | 80 | 20 | No | - | 0%
Anorthosite | Al | 70 | 30 | Yes, no propagation | - | 0%
Anorthosite | Al | 60 | 40 | Yes | Slow | 80%
Anorthosite | Al | 50 | 50 | Yes | Slow | 80%
Enstatite | Al | 80 | 20 | No | - | 0%
Enstatite | Al | 70 | 30 | No | - | 0%
Enstatite | Al | 60 | 40 | Yes, no propagation | - | 0%
Enstatite | Al | 50 | 50 | Yes, no propagation | - | 0%
LMS-1 | Mg | 74 | 26 | Yes | Fast | 90%
LHS-1 | Mg | 74 | 26 | Yes | Fast | 90%
Notes: Hot wire in atmosphere.
Dependency from moisture in the mixture. A specific procedure was set up.
LHS/LMS ignition but in some cases no propagation. Propagation is better close to the stoichiometric. LMS better than LHS
Same for anorthite
Enstatite (bronzite) almost no propagation.
Magnesium provided a fast propagation.
Results are doped by the presence of atmosphere that acts as catalyst with the oxygen reacting with alumimun in a strong exothermic reaction that enhance the propagation.

## Slide 13: Proof of Concept - Laser Ignition
Notes: laser diode (5W, 405 μm)
LMS/Al 60/40
Better selection of the laser (higher power, wavelength tuned on the type of reactants).

## Slide 14
BREADBOARD DESIGN

## Slide 15: System Design: Mission Objectives
Requirement | Description | Rationale | Comment
ACME-MIS-001 | The ACME breadboard shall demonstrate the increase of TRL of the concept to 4. | Compliant with main programmatic target for the “Technological Demonstration” stage required by OSIP. | Definition based on ECSS-E-HB-11A.
ACME-MIS-002 | The ACME breadboard shall be able to test the performance of thermite reactions as lunar night survival system in conditions consistent with results of the Proof of Concept in laboratory environment. | Maana wants to gain deeper knowledge about the performance potentially achievable though this concept. This data is intended to be used to better tackle the commercialization of the system in the short term. | Definition of “laboratory environment” based on ECSS-E-HB-11A.
ACME-MIS-003 | The ACME breadboard shall be able to test the performance of the laser ignition in laboratory environment. | To validate the choice of using a laser system as ignition method for the thermite reaction, the breadboard must be designed having in mind performance optimization. This performance must be then measured and validated. | Definition of “laboratory environment” based on ECSS-E-HB-11A.
ACME-MIS-004 | The ACME breadboard shall be able to test the performance of metal production from regolith simulant in laboratory environment. | Through thermite reaction, it is possible to extract pure metals from the oxides naturally contained in the regolith. It is important that the breadboard allows Maana to investigate what are the products of the thermite reaction for various conditions and therefore outline experimental limits for the performance of this process. | Definition of “laboratory environment” based on ECSS-E-HB-11A.

## Slide 16: System Design: Functional Analysis
REACTION CHAMBER
BUFFER TANK
F2.1
F6.6
F2.2

## Slide 17: System Design: Functional Analysis
REACTION CHAMBER
BUFFER TANK
F3.1
F3.2
F3.3
F6.1
F6.2
F3.4
Energy released by reaction | 
Instant thermal power absorbed | 
Energy released by reaction | 
Instant thermal power absorbed | 

## Slide 18: System Design: Functional Analysis
REACTION CHAMBER
BUFFER TANK
F1
F6.5

## Slide 19: System Design: Functional Analysis
REACTION CHAMBER
BUFFER TANK
F5.2
F5.1

## Slide 20: System Design: Functional Analysis
REACTION CHAMBER
BUFFER TANK
F4.4
F4.2
F4.3
F4.1

## Slide 21: Design - Reaction Chamber
Reaction Chamber
1 – Inlet and outlet liquid feedthroughs
2 – Backup viewport
3 – Chamber cover handling
4 – Inlet ball valve
5 – Pressure gauge
6 – Outlet ball valve
7 - Electric feedthroughs
8 - Spare vacuum connection
9 - Chamber core handling

## Slide 22: Design - Reaction Chamber
Reaction Chamber
11 – Thermocouple feedthrough
12 – Safety pressure valve
13 – Camera viewport
14 – Laser viewport
15 – Copper spiral
16 – Alumina crucible
17 – Buffer layer
18 –Insulation

## Slide 23: Design - Buffer Tank
Buffer Tank
1 - Temperature sensor PT100
2 - DC motor
3 - Push-in Connector
4 - Top cover handling
5 - Drainage valve
6 - Stirring propeller
7 - Inlet pipe
8 - Insulation
9 - Outlet pipe

## Slide 24: Design - Laser Unit
Setup
Starting laser (T0)
Ignition (T0+20s)
Thermite
Ignition
( LMS-1/Al @Maana)
Aluminum
Melting
(Al dust @supplier)
Melting
Aluminum powder
Molten particles
Experiments confirms ignition with FC-W-808nm-40W-DJ01163 by CNI Laser
Specifications: 808 nm with power rating 10-40 W

## Slide 25: Breadboard integration
BUFFER TANK
LASER COLLIMATOR
CAMERA
WATER LOOP INLET
WATER LOOP OUTLET
VACUUM PUMP EXHAUST
VENTING EXHAUST

## Slide 26: Functional verification
Chart: Time [s]
1
3
2
Performed 14 functional tests. Identified 3 NC:
Ineffective monitoring of reaction front
Long time to thermalization
Low performance of heat transfer
Performance tests with different configurations to identify root-cause
Notes: Alumina crucibles are not able to contain violent reactions. Crucible in graphite can resist to extremely violent reactions (Ilmenite/Aluminum) and are selected for future tests.
Thermocouple at the bottom of the crucible is not a good indicator for monitoring the advancement of the reaction. This parameter will not be further investigated in a quantitative manner for future tests.
The position of the third temperature sensor is too high and cannot be used unless the Water Tanks is full. The Tanks was modified to lower the position of the thermocouples.
Excessively long time required to arrive to thermalization between the water and the crucible and the water tank losses are too high to have precise derivation of equilibrium conditions. A further performance analysis on heat acquisition and transfer was set-up to investigate root cause of this problem.
At equilibrium, the energy stored in the water is only 50% of the theoretical one. Performance tests with different configurations to identify root-cause

## Slide 27: Performance verification
Chart: Time in s
Chart: Time in s
Notes: Baseline configuration has extremely poor performance and cannot be used for further tests.
The use of a copper jacket promotes the heat transfer and peak temperature is higher. It does not prevent heat losses and therefore the asymptotic temperature is same as baseline.
The use of top insulation slows down heat loses and therefore we have higher peak temperature. It also prevent the heat to escape to the un-insulated cover of the vacuum chamber and therefore it gives higher equilibrium temperature.
The use of both top-insulation and copper jacket largely increase both peak and equilibrium temperatures. This is indeed the recommended configuration.
Vacuum shows similar relative results. The only difference is on the behavior of the top-insulation, which does not prevent convective losses (no air).
It is proven that at low temperatures the presence of air promotes the heat exchange with the spiral and general performance if properly insulated on top.

## Slide 28
BREADBOARD TESTING

## Slide 29: Samples and simulants
Step | Description
#01 | Proper regolith simulant taken accordingly to test description
#02 | Proper amount of beneficiated-regolith taken (option, depending on test description) accordingly to test description
#03 | Proper metallic powder taken accordingly to test descripion
#04 | Thermite mixture mixed in correct proportion accordingly to test description
#05 | Thermite dispensed to plastic pot
#06 | Manual mixing
#07 | Samples placed on Digital Roller mixed Mixing speed set-up: 70 RPM Duration set-up: 6h
#08 | Holes made on pots cap
#09 | Pots placed in desiccating vacuum chamber with presence of new batch of calcium chloride
#10 | 40Pa Vacuum created
#11 | 24h of drying time kept
#12 | Replace calcium chloride pot
Bulk mineralogy of LHS-1 before and after beneficiation [wt%]
Samples preparation procedure
Oxides | Raw | Benef.
SiO2 | 51.2 | 44.2
CaO | 12.8 | 8.5
Al2O3 | 26.6 | 19.5
MgO | 1.6 | 4.1
K2O | 0.5 | 1.6
Fe2O3 | 2.7 | 12.0
Cumulative size distribution of LMS-1 against Apollo samples
The testing campaign will use mixtures of Aluminium with mineralogically and granulometrically accurate simulants:
LMS-1 (Mare) is the standard for calibration and performance confrontation.
LHS-1 (Highland) is used to compare the H/M use cases in terms of performance.
Beneficiated simulant is added to standard (LMS-1) to correlate increase in performance.

## Slide 30: Ignition method: heating wire
Chart: Time [s]

## Slide 31: Ignition method: laser
Chart: Time [s]

## Slide 32: Ignition method: troubleshooting
Root-cause | Experiment | Outcome
Improving kinetic of reaction | Oxide mixtures instead of LMS-1 simulant | ✘
 | LMS-1/Al with ball-milled regolith | ✘
 | LMS-1/Al with aluminum flakes | ✘
Improving energy of reaction | LMS-1 replacing Al with Mg | ✘
 | LMS-1/Al changing mixing ratios | ✘
 | Replacing LMS-1 with beneficiated-LMS | ✘
 | Replacing LMS-1 with Ilmenite | ✓
Lowering activation energy | LMS-1/Al with pre-heating | ✓

## Slide 33: Ignition method: ilmenite
Pure Ilmenite/Al mixtures propagate for large spectrum of mixture ratios
(70/30wt% on left, 60/40wt% on right)
Can withstand impurities of LMS-1 up to 20% of the total ilmenite content
(35/35/30wt% on left, 14/56/30wt% on right)

## Slide 34: Ignition method: pre-heating
Chart: Time [m]
 | 0 | 1400
 | 0 | 1400
 | 0 | 1400
 | 0 | 1400

## Slide 35: Mixture ratio: LMS and LHS
Composition LMS-1/Al wt% | 75/25 | 70/30 | 60/40 | 50/50
Iteration 1 | 27% | 22.5% | 25% | 14%
Iteration 2 | 15% | 25% | 32.5% | 9.5%
Iteration 3 | 29.5% | 33.5% | 22.5% | 5.5%
Average | 23.8% | 27% | 26.7% | 9.7%
Composition LHS/Al wt% | 60/40 | 70/30
Iteration 1 | 4.5% | 11%
Iteration 2 | 6.5% | 14%
Iteration 3 | 8.5% | -
Average | 6.5% | 12.5%
Tests on 20g samples w/o ball-milling, w/ pre-heating procedure

## Slide 36: Mixture ratio: ilmenite
Self-ignited slow reaction with 70/30wt% mixing ratio
Tests on 20g samples w/o ball-milling, w/ pre-heating procedure
Grinded products with magnetic behavior
Products of violent reaction after laser ignition

## Slide 37: Large samples ignition
Chart: Time [m]
Slow heating procedure
53% propagation, 780°C max T

## Slide 38: Large samples ignition
Fast heating procedure
full propagation, 1137°C max T
Chart: Time [m]

## Slide 39: XRD analysis of LMS-1/Al 70/30 products
50g LMS-1/Al 70/30wt%
full propagation, 1137°C
Samples have been turned into a fine powder using a hydraulic press. Preliminary observation of XRD analysis carried on the products of the reaction allowed to identify Si as the only pure metal.
The presence of Si could explain why poor propagation and energy release of the thermite were experienced. Supplement of analysis of the samples is ongoing.
Other species are compatible with partially unreacted thermite.
39

## Slide 40: XRD analysis of ILM/Al 70/30 products
Samples have been turned into a fine powder using a ball milling machine. Preliminary observation of XRD analysis carried on the products of the reaction allowed to identify Al-Ti and Al-Fe alloys as separate products.
Al-Fe are highly magnetic (as verified inhouse) and can be separated and potentially used for additive manufacturing.
Al-Ti is not magnetic. Ti could be obtained by thermal segregation (i.e. directional solidification) and used in a pure form for additive manufacturing.
Al2O3 corundum is an impurity introduced by ball-milling.
40
20g ILM/Al 70/30wt%
magnetic grinded products

## Slide 41
NEXT STEPS

## Slide 42: ACME development roadmap
Proof-of-Concept and first lab scale demonstration
IMPLEMENTED THROUGH OSIP (03/2022 – 08/2023)
Budget: 175k€
Phase 0/A of ACME tech demonstrator and Proof-of-Concept and lab scale integration of integrated concept
IMPLEMENTED THROUGH GSTP ELEMENT 1 (2024 - 2025)
Budget: 700k€ (TBC)
Phase B/C/D of ACME tech demonstrator
IMPLEMENTED THROUGH GSTP ELEMENT 2 (2025 - 2028)
Budget: 7.6M€ (TBC)
Phase E/F of ACME tech demonstrator
IMPLEMENTED THROUGH GSTP ELEMENT 3 (2028 - 2029)
Budget: TBD
Phase A/B/C/D of ACME plant
(2029 - 2033)
Budget: TBD
Phase E/F of ACME CL plant
(2034 - 2035)
Budget: TBD
42

## Slide 43: ACME GSTP proposal
PART A
Breadboard modifications and testing
(*) Potentially implemented as part of an OSIP or GSTP Element-1 De-risk
PART B
Phase 0/A
ACME demonstrator
Phase B/C/D of ACME tech demonstrator
43
PART C
ACME integrated concept PoC
PART D*
Additive manufacturing PoC

## Slide 44: Conclusions
44
A first experimental proof of the ACME concept was achieved using laser ignition in vacuum conditions.
The current experimental setup requires some modifications to allow more accurate thermal acquisition and full calorimetric characterization.
Several thermite reactions have been obtained from raw regolith simulants or its beneficiated forms in vacuum conditions at different mixing ratios.
Two reactions (LMS-1/Al and ILM/Al) have been identified as of potential interest for generation of heat using metallothermic reaction.
LMS-1/Al reaction proved to be more interesting in the perspective of a larger ISRU architecture given the higher abundance of raw regolith.
The ILM/Al proved to be able to generate higher energy and products (Al-Ti and Al-Fe alloys) that could be further processed and used in additive manufacturing applications, but it has to deal with lower abundance of ilmenite.
Pre-heating of the reactants enhanced the ignition and the propagation of the reactions.
Pre-processing of the reactants may have some effect on the ignition and propagations of the reactions.
A first “closed loop” architecture has been identified but needs to be validated through further testing.