## Slide 1: ASSESSMENT OF AUTOMOTIVE EEE COMPONENTS SUITABILITY FOR SPACE APPLICATIONS
Final presentation

## Slide 2: tABLE OF CONTENTS
Agenda
1
WP1 - AEC-Q Automotive
Part Selection
2
WP2 – Comp. of automotive and Space Approval Testing
3
WP3 - Tests
4
WP4 - Recommendations
5

## Slide 3: agenda
WP1 - AEC-Q Automotive part Selection (L. de Pablo, TAS-E)
WP2 - Comparison of automotive and Space Approval Testing (L. de Pablo, TAS-E)
Break
WP3 - Test Campaign (F. Waldron, Tyndall National Institute
WP4 – Conclusions and Recommendations (L. de Pablo, TAS-E)

## Slide 4: WP4 – final recommendations
RECOMMENDATIONS
  Procure recent lots (DC<3 years), store in controlled conditions (ideally dry N2).
  Conduct periodic visual inspection on stored samples.
  Carefully follow-up of PCN/PDN
  Carry out always Constructional Analysis, not unusual to see delaminations on AEC-Q devices, and discuss results with manufacturer (TAS’ experience)
  Carry out detailed CA, materials analysis, Tg, CTE, etc. on samples of any new lots to ensure similarity with previous lots. Outgassing almost never fail (TAS’s experience), but should be done on 1st lot and then could help to ensure similarity.
  Verify the manufacturer’s AEC qualification data & PPAP (could be as old as 10 years +: TAS’ experience).
  For grade‐1 applications, full qualification needed on 1st lot (AEC‐Q parts), then periodic test (e.g. every 2 years life test).
  For grade‐2 & 3 mission applications, CA only minimum (unless AEC qualification data is very old or CA findings).
  SnPb re‐tinning may not be required for some applications, (JESD‐201 class 2 recent data & other measures such as coatings, barrier layers, etc..)

## Slide 5: Possible extended works - proposal
TESTING ON REMANING SAMPLES OF EXISTING LOTS
TESTING ON NEW SELECTED TYPES
OTHER
  STUDIES
  AUDITS
  MARKET SURVEY UPDATE

## Slide 6: TESTING ON REMANING SAMPLES OF EXISTING LOTS
  Rationale:
    For Op Amp, we can compare TID on virgin parts and Life Tested parts
  Rationale:
    Literature show Effective Tg (& CTE) dependence on moisture absorption. It could also show slight dependence on thermal fatigue and ageing (hypothesis)
    Then Outgassing could also be dependent on ageing, thermal fatigue and long term moisture environment (hypothesis)
  EIA JEDEC JESD22-A110D for HAST

## Slide 7: TESTING ON REMANING SAMPLES OF EXISTING LOTS
  Rationale:
    Capacitors are soldered onto board and boards submitted to HTOL, THB & 500 thermal cycles.
    Dependence of cracking and delamination with TC and also HTOL & THB to be checked by Acoustic Microscope and Microsection (not seen on 3pcs after 500 thermal cycles)
    Correlation of C.SAM & uSection views at board level
    Some pieces (or all) could be intentionally stressed with solder iron to simulate improper repair

## Slide 8: TESTING ON new selected types – HEAVY IONS
  Rationale: on MOSFET we saw that
    SEE SOA could be dramatically affected by sample size (typically 2 only)
    Variability due to burn-in or not burn-in
  Hypothesis: similar feature (sample-size & burn-in effect on schottkies) as SEB depends on barrier height

## Slide 9: TESTING ON new selected types – HEAVY IONS
  Rationale: on MOSFET we saw that
    SEE SOA could be dramatically affected by sample size (typically 2 only)
    Variability due to burn-in or not burn-in
  Hypothesis: similar feature (sample-size & burn-in effect on schottkies) as SEB depends on barrier height

## Slide 10: Other: studies, audits, market survey
  AUDITS / MARKETYS SURVEY: questionnaire to be filled by some tens of manufacturers
  SPECIFIC STUDIES: Automotive system, trends, evolution, new standard test methods, new manufacturers etc..