## Slide 1
Plasma Bound De-Risk Project Final Presentation
13th of May 2024

## Slide 2
Project Proposal
01
Controlled Polymer Ablation Overview
02
WP2000 – Space Market Analysis
03
Presentation Outline
WP3000 – Qualification Approach
04
WP4000 – Test Campaign
05
WP5000 – Follow-On Activity Planning
06
Conclusion
07
2

## Slide 3
Project: Assessments to Prepare and De-Risk Technology Developments Framework (G617-241TA) –
Controlled Polymer Ablation (CPA).
Background: PlasmaBound is the sole provider of CPA - technology for enhanced adhesive bonding.
Scope: Development of CPA to TRL 4 for composite-to-composite bonding activities for space applications.
Timeline: 9 Months
Contractor: PlasmaBound Ltd.
Contractee: ESA
Supports: ÉireComposites Teo.
Composites Testing Laboratory Teo.
Mecano-ID
Proposal – January 2021
PLASMA BOUND
Notes: General Support Technology Programme (GSTP) ESA

## Slide 4
Highly reactive species like ions, electrons and radicals.
Breaks the chemical bonds within the polymer, leading to the dissociation of polymer molecules.
Controlled Polymer Ablation Overview
Fibre Weave
Polymer
CPA Plasma Plume
Contaminant
Revealed Fibres

## Slide 5
PLASMA BOUND
WP2000 – Space Market Analysis
D1 – Supply Induced Obsolescence Report
Supply & Demand:
Plasma device agnostic
Atmospheric plasma widely used
Rare Earth Materials:
  Hafnium in electrode
  EU is net exporter of Hafnium
5

## Slide 6
PLASMA BOUND
WP2000 – Space Market Analysis
Pg 221
D2 – Regulation Induced Obsolescence Report
  ECSS Compliance:
  “creation, or exposure, of a new surface”
  REACh Compliance:
  CPA add-on
  Air & Electricity consumed
  Waste exempt
RoHs Compliance:
CE marked device
6
Notes: Registration, Evaluation, Authorisation and Restriction of Chemicals
Restriction of Hazardous Substances Directive

## Slide 7
PLASMA BOUND
WP2000 – Space Market Analysis
D3&4 – Preliminary Technical Requirements Specifications & Breadboard Design Concepts
Technical Requirements:
Materials Selection
SotA preparation methods
Joint performance testing
Breadboard Design Concepts
7

## Slide 8
PLASMA BOUND
WP3000 – Qualification Approach
Adhesive Bonding with EA9695 Film & ALU5052 Honeycomb
NDT
NDT
Peel Ply
CPA
Skin CFRP
Specimen Machining
Standardised Testing
Adhesive Bonding with EA9394 Paste
NDT
NDT
Mechanical Abrasion
ECSS-E-HB-32-21A
CPA
Monolithic CFRP
Specimen Machining
Standardised Testing
8
D5 – Verification Plan
Storage Time Assessment
ISO 8 Clean Room Suitability Assessment
Verification Programme Matrix
Notes: Add full TS matrix in additional slides at the end. Ready for questions
Ver Table

## Slide 9
PLASMA BOUND
WP3000 – Qualification Approach
D6 – Breadboard Design Definition for Function Performance Verification
9
Notes: The chosen space applications for monolithic CFRP are principally solar arrays and large satellite/platform primary structures with opportunities to expand to satellite primary structures with integrated mirror.
Figure 2‑4: CFRP Splice-Joint with adhesive bonding between both the skin to honeycomb core (green) and skin to splice plate, with Loctite EA9695 (skin to honeycomb) and Loctite EA9394 (skin to splice plate) adhesive applied (both represented in red). Note: the splice span is shortened for illustration purposes only.

## Slide 10
PLASMA BOUND
WP4000 – Test Campaign
Chart: ESA_UD EXCF Monolithic_T1 Surface Free Energy
| Adhesive | Abrasion | S.O.1 | S.O.2 | S.O.3 | S.O.4 | S.O.5 | S.O.6 | S.O.7 | S.O.8
Dispersive [mN/m] | 44.01 | 45.2 | 32.54 | 30.61 | 30.15 | 31.76 | 29.97 | 35.22 | 32.3 | 32.42
Polar [mN/m] | 0.053 | 0.18 | 37.52 | 42.99 | 40.55 | 41.33 | 41.16 | 37.01 | 38.46 | 38.48
D7 – Optimisation Process Parameters
6 Treatment Variables
DoE, SFE, Pull-off tests, Adhesive ST, Microscopy
10
Notes: New: Gas Flow, [Plasma Frequency], Power, Modulation/PCT, Nozzle Height, Treatment Speed, Raster Gap.

## Slide 11
PLASMA BOUND
WP4000 – Test Campaign
Sandwich Bond Joints
Toray RS36 AFC 49 M55JB 6K 200g 36% 0.3m
4-ply lay-up, 0.8mm thick [0/+45/-45/0°]
Loctite EA9695 Aero Epoxy Film Adhesive
Easy Composites ALU5052 (3.2mm cells, 15mm thickness)
Monolithic Bond Joints
Toray RS36 AFC 49 M55JB 6K 200g 36% 0.3m
8-ply lay-up, 1.6mm thick [0/+45/-45/90° | 90/-45/+45/0°]
16-ply lay-up, 3.2mm thick [0/+45/-45/90° | 90/-45/+45/0° | 0/+45/-45/90° | 90/-45/+45/0°]
Loctite EA9394 Aero Epoxy Paste Adhesive
D8.1 – Manufacturing Phase Report
11
Notes: Figure 4‑32: Assembled FWT Panels – Date Scanned 05/01/2023 (Main dB Range: 21-31dB).

## Slide 12
PLASMA BOUND
WP4000 – Test Campaign
Chart: Treatment Type
| Peel Ply | CPA Depth 1 | CPA Depth 2 | CPA Depth 3 | CPA Depth 4 | CPA Depth 5
 | 3.2387 | 3.5116 | 3.7726 | 3.9064 | 4.0942 | 3.551
D8.2 – Optimisation Test Report
Monolithic: SLS
Skin: FWT, CDP
FWT: CPA Depth 4
SLS: CPA E
CDP
12
Notes: Non-Standard Failure Mode for CDP Testing. The composite skin snapped.

## Slide 13
PLASMA BOUND
WP4000 – Test Campaign
D8.3 – Experimental Test Report
Monolithic: DLS Skin: FWT Skin: SFL
13

## Slide 14
PLASMA BOUND
WP4000 – Test Campaign
D8.3 – Experimental Test Report
Monolithic: DLS after Storage Skin: FWT after Storage
14

## Slide 15
PLASMA BOUND
WP4000 – Test Campaign
D9 – Breadboard Test Report
Sandwich Panels joined by
Monolithic Splice Plates
Chart: Face Bending Stress (MPa) vs Treatment Type
| Peel Ply & Hand Sand | CPA Partial Reveal
 | 309.71 | 380.45
n = 2
15
Notes: The chosen space applications for monolithic CFRP are principally solar arrays and large satellite/platform primary structures with opportunities to expand to satellite primary structures with integrated mirror.
Figure 2‑4: CFRP Splice-Joint with adhesive bonding between both the skin to honeycomb core (green) and skin to splice plate, with Loctite EA9695 (skin to honeycomb) and Loctite EA9394 (skin to splice plate) adhesive applied (both represented in red). Note: the splice span is shortened for illustration purposes only.

## Slide 16
PLASMA BOUND
WP5000 – Follow-On Activity Planning
D10 – Developmental Plan – CPA to TRL 6
16

## Slide 17
PLASMA BOUND
WP5000 – Follow-On Activity Planning
TRL 4 & 5 for Satellite Struts with Mecano ID
TRL 5 for Sandwich Structure Breadboard
TRL 6 Engineering Models (Partner and application needed for sandwich structure)
17
Notes: Discuss Realtra with Nick, set up a comment on it

## Slide 18
PLASMA BOUND
Conclusion
Objectives Achieved
TRL 3: Achieve Proof-of-Concept, address regulatory & obsolescence factors
TRL 4: Elemental Testing & Breadboard Testing
18

## Slide 19
PLASMA BOUND
Deliverables
Doc ID | Deliverable Title | Milestone | Description of documents
D1 | Supply Induced Obsolescence Report | WP2000 | Investigate potential future supply chain adjustments.
D2 | Regulation Induced Obsolescence Report | WP2000 | Investigate potential future regulatory adjustments.
D3 | Preliminary/ Technical Requirement Report | WP2000 | Investigate functional performance requirements
D4 | Conceptual design of the Element (Breadboard Design) | WP2000 | Includes in-depth context for CPAs opportunities within space.
D5 | Validation and Verification Plan | WP3000 | Describing the purpose, goal and scope of testing for elevation to TRL 4.
D6 | Breadboard design definition for the functional performance verification | WP3000 | A description of the Monolithic and Sandwich Breadboards Justification for both breadboards against the application chosen.
D7 | Optimisation Process Parameters | WP4000 | Details of internal CPA optimisation activities(BIPR Concerned)
D8.1 | Manufacturing Phase Report | WP4000 | Manufacturing details.
D8.2 | Optimisation Test Report | WP4000 | Testing details. Wide range of CPA treatments (x10).
D8.3 | Experimental Test Report | WP4000 | Testing details. Narrowed range of CPA treatments (x3).
D9 | Breadboard Test Reports | WP4000 | Testing details. Breadboard testing on single CPA treatment type (x1).
D10 | Developmental Plan – CPA to TRL 6 | WP5000 | Details of activities for bringing PlasmaBound’s CPA solution to TRL 6.

## Slide 20
PLASMA BOUND
Project Schedule
Project KO
May ‘21
Supply & Regulation Induced Obsolescence Reports
June ‘21
Verification & Validation Plan
August ‘21
Breadboard Design
September ‘21
PB Optimisation Lab Work September ‘22
Breadboard Testing
January ‘24
Developmental Plan to TRL 6
January ‘24
Project Acceptance
May ‘24
CTL Testing Begins
October ‘22
ÉireComposites Manufacturing Begins
January ‘22
ÉireComposites Manufacturing Ends
May ‘23
Sources of Schedule Delay:
Global supply chain issue 2021 Difficulty obtaining project materials
Curing Cycle Issues – ÉireComposites Concern over curing cycles in 2023 led to investigation of all production
Bonding issues – CTL NDT detected large voids in SLS paste bond joints, after testing and investigation these were found to be false NDT readings
Manpower – Plasma Bound Balancing long term projects with short term opportunities